Supporting Information

Microbubbles Decorated with Dendronized Magnetic Nanoparticles for Biomedical Imaging. Effective Stabilization via Fluorous Interactions

Da Shi, Justine Wallyn, Dinh-Vu Nguyen, Francis Perton, Delphine Felder-Flesch, Sylvie Bégin-Colin, Mounir Maaloum, Marie Pierre Krafft*

Figure S1. Infrared spectra of IONPs covered by oleic acid (grey), or dendronized with C2H5OEG8Den (black), C2F5OEG8Den (red), C4H9OEG8Den (orange) and C4F9OEG8Den (blue).

Figure S2. Hydrodynamic diameter distributions of IONPs covered with oleic acid  (10  1 nm), in suspension in THF aqueous dispersions (0.05 mg mL-1).

Figure S3. Variation of the interfacial tension of the gas/aqueous phase interface as a function of time under air (black) and under F-hexane-saturated air (red). Temperature was 25°C.