Electronic Supplementary Information

Non-labeled and highly sensitive probe detection with novel hierarchical SERS substrates fabricated by nanoindentation and chemical reaction methods

Jingran Zhang*1, Tianqi Jia*1, Yongda Yan2, Li Wang3, Peng Miao4, Yimin Han*5, Xinming Zhang1, Guangfeng Shi1, Yanquan Geng2, Zhankun Weng1, Daniel Laipple3, Zuobin Wang1

1 Ministry of Education Key Laboratory for Cross-Scale Micro and Nano Manufacturing, Changchun University of Science and Technology, Changchun 130022, China

2 The Key Laboratory of Micro-systems and Micro-structures Manufacturing of

Ministry of Education, Harbin Institute of Technology, Harbin, Heilongjiang 150080, P.R. China

3 Institute of Materials Research, Helmholtz-Zentrum Geesthacht, Max-Planck-Strasse 1, Geesthacht, D-21502, Germany

4 School of Chemistry and Chemical Engineering, Harbin Institute of Technology, Harbin, Heilongjiang 150010, P.R. China

5 Department of Gynaecology, No. 3 Subsidiary Hospital, Harbin Medical University, Harbin, Heilongjiang, 150040, P. R. China

* Corresponding author. Tel.: +86-0451-86298932

E-mail address: hanyimin@163.com (Y.M. Han)

* Corresponding author. Tel.: +86-0431-85582420

E-mail address: zhangjingran@cust.edu.cn (J. R. Zhang)

Supplementary Figures and Tables

Figure S1 (a)SEM image of Ag/Cu surface in AgNO3 solution with 5 minutes (b) EDS image of Ag/Cu surface in AgNO3 solution with 5 minutes.

Table S1 the table of elements consitute of Ag/Cu surface

| Element | Quality percentage (%) | Molecular percentage(%) |
| --- | --- | --- |
| C | 5.95 | 19.72 |
| O | 11.73 | 29.17 |
| Cl | 1.01 | 1.13 |
| Cu | 80.65 | 49.63 |
| Ag | 0.66 | 0.35 |
| total | 100 | 100 |

Figure S2 (a)SEM image of the arrayed triangular cavities with fx=5μm、fy=1μm in AgNO3 solution with 5 minutes (b)SEM image of the plie-ups of cavities with fx=5μm、fy=1μm in AgNO3 solution with 5 minutes (c)EDS image of the arrayed cavities with fx=5μm、fy=1μm (d) EDS image of the plie-ups of cavities with fx=5μm、fy=1μm.

Table S2 The table of elements consitute of internal cavities for the hierarchical SERS substrate with the machining feed of fx=5μm、fy=1μm

| Element | Quality percentage(%) | Molecular percentage(%) |
| --- | --- | --- |
| C | 8.93 | 29.29 |
| O | 7.80 | 19.21 |
| Cu | 82.65 | 51.27 |
| Ag | 0.62 | 0.23 |
| total | 100 | 100 |

Table S3 The table of elements consitute of pile-ups of cavities for the hierarchical substrates with the machining feed of fx=5μm、fy=1μm

| Element | Quality percentage(%) | Molecular percentage(%) |
| --- | --- | --- |
| C | 7.51 | 26.60 |
| O | 7.21 | 19.18 |
| Cu | 74.84 | 50.11 |
| Ag | 10.43 | 4.11 |
| total | 100 | 100 |

Figure S3 (a)SEM image of the arrayed triangular cavities with fx=2μm、fy=2μm in AgNO3 solution with 5 minutes (b)SEM image of the plie-ups of pyramid cavities with fx=2μm、fy=2μm in AgNO3 solution with 5 minutes (c)EDS image of the arrayed triangular cavities with fx=2μm、fy=2μm (d) EDS image of the plie-ups of pyramid cavities with fx=2μm、fy=2μm.

Table S4 The table of elements consitute of internal cavities for the hierarchical SERS substrate with the machining feed of fx=2μm、fy=2μm

| Element | Quality percentage(%) | Molecular percentage(%) |
| --- | --- | --- |
| C | 6.57 | 23.07 |
| O | 7.63 | 20.12 |
| Cu | 85.16 | 56.56 |
| Ag | 0.64 | 0.25 |
| Total | 100 | 100 |

Table S5 The table of elements consitute of pile-up of cavities for the hierarchical SERS substrate with the machining feed of fx=2μm、fy=2μm

| Element | Quality percentage(%) | Molecular percentage(%) |
| --- | --- | --- |
| C | 7.36 | 23.07 |
| O | 6.41 | 20.12 |
| Cl | 0.18 | 0.22 |
| Cu | 75.79 | 51.71 |
| Ag | 10.25 | 4.12 |
| total | 100 | 100 |

Figure S4 (a)SEM image of the arrayed triangular cavities with fx=5μm、fy=5μm in AgNO3 solution with 5 minutes (b)SEM image of the plie-ups of pyramid cavities with fx=5μm、fy=5μm in AgNO3 solution with 5 minutes (c)EDS image of the arrayed triangular cavities with fx=2μm、fy=2μm (d) EDS image of the plie-ups of pyramid cavities with fx=5μm、fy=5μm.

Table S6 The table of elements consitute of internal cavities for hierarchical SERS substrate with the machining feed of fx=5μm、fy=5μm

| Element | Quality percentage(%) | Molecular percentage(%) |
| --- | --- | --- |
| C | 7.98 | 28.07 |
| O | 5.54 | 14.62 |
| Cu | 85.72 | 57.01 |
| Ag | 0.77 | 0.3 |
| total | 100 | 100 |

Table S7 The table of elements consitute of pile-up of cavities for hierarchical SERS substrate with the machining feed of fx=5μm、fy=5μm

| Element | Quality percentage (%) | Molecular percentage (%) |
| --- | --- | --- |
| C | 7.49 | 27.61 |
| O | 4.38 | 12.12 |
| Cu | 84.11 | 58.62 |
| Ag | 4.03 | 1.65 |
| total | 100 | 100 |

Table S8. Parameters of the feeds in the X-Y directions for fabrcating micro/nanostructures on the Cu(110) surface

|  | (1) | (2) | (3) | (4) | (5) | (6) | (7) | (8) | (9) | (10) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| fx(μm) | 10 | 5 | 5 | 5 | 5 | 5 | 2 | 2 | 2 | 2 |
| fy(μm) | 10 | 5 | 4 | 3 | 2 | 1 | 4 | 3 | 2 | 1 |

Figure S5 (a) Raman spectrum of R6G molecules of 10-8mol/L with different feeds on the Ag/Cu substrates with the corrosion time of 5minues (b) Average Raman intensity of R6G of the 1362cm-1 peak for the structured Ag/Cu substrates with different feeds.

Figure S6 (a) Raman spectra of R6G molecules of 10-8mol/L with different feeds on Ag/Cu substrates with the corrosion time of 10minues. (b) Average Raman intensity of R6G of the 1362cm-1 peak for the Ag/Cu substrates with different feeds.

Figure S7(a) Electric field distribution of a Ag nanoparticle with a radius of 100nm on the air (b) Electric field distribution of a Ag nanoparticle with a radius of 100nm on substrate.