Supporting Information

Particle size effect in the mechanically assisted synthesis of -cyclodextrin mesitylene sulfonate

Stéphane Menuel, Sébastien Saitzek, Eric Monflier, Frédéric Hapiot*

Univ. Artois, CNRS, Centrale Lille, Univ. Lille, UMR 8181 – UCCS – Unité de Catalyse et Chimie du Solide, F-62300 Lens, France.

|  | Page |
| --- | --- |
| Determination of  | 2 |
| Solid-state kinetics models | 3 |
| General procedure for the synthesis of mono-6-O-(2-mesitylenesulfonyl)--cyclodextrin | 5 |

Determination of 

α=ntn∞

 is defined by:  		with nt  the conversion at time t, and n the final conversion.

Fig. S1 Compared values of  against time in the synthesis of -CDMts without grinding -CD () and with ground -CD (~235 nm) ().

Fig. S2 Compared values of  against time in the synthesis of -CDMts in the presence of KOH (1 equiv. with respect to -CD) without grinding -CD () and with ground -CD (~235 nm) ().

Solid-state kinetics models

Table S1 Solid-State Rate and Integral Expressions for Different Reaction Models.

| Model | Abbreviation | Integral form: g() = k.t |
| --- | --- | --- |
| nucleation models |  |  |
| power law | P2 | 1/2 |
|  | P3 | 1/3 |
|  | P4 | 1/4 |
| Avrami-Erofeev | A2 | [-ln(1-)]1/2 |
|  | A3 | [-ln(1-)]1/3 |
|  | A4 | [-ln(1-)]1/4 |
| Prout-Tompkins | B1 | ln[/(1-)] + ca |
| geometrical contraction models |  |  |
| contracting area | R2 | 1-(1-)1/2 |
| contracting volume | R3 | 1-(1-)1/3 |
| diffusion models |  |  |
| 1-D diffusion | D1 | 2 |
| 2-D diffusion | D2 | ((1-)ln(1-))+ |
| 3-D diffusion-Jander | D3 | (1-(1-)1/3)2 |
| Ginstling-Brounshtein | D4 | 1-(2/3)-(1-)2/3 |
| reaction-order models |  |  |
| zero-order | F0/R1 |  |
| first-order | F1 | -ln(1-) |
| second-order | F2 | [1/(1-)]-1 |
| third-order | F3 | (1/2)[(1-)-2-1] |

a Constant of integration.

Table S2 Solid-state kinetics model for the synthesis of -CDMts without base.

Table S3 Solid-state kinetics model for the synthesis of -CDMts in the presence of KOH (1 equiv. with respect to -CD).

General procedure for the synthesis of mono-6-O-(2-mesitylenesulfonyl)--cyclodextrin

-cyclodextrin (1500 mg, 1.32 mmol) and 2-mesitylenesulfonyl chloride (290 mg, 1.32 mmol) were placed in a 10 mL zirconium oxide reactor containing one zirconium oxide ball of 9 mm diameter. The solid mixture was shaken for 5 min at 30 Hz. Shaking was then stopped for 5 min. The procedure was repeated 54 times for a total grinding time of 270 min. The reactor was opened every 3 cycles to limit agglomeration of the powder. The resulting powder was purified by flash chromatography on silica gel using acetonitrile/water (9/1 to 8/2 v/v) as mobile phase. Isolated yield 21% (364mg). 1H NMR (300 MHz, DMSO-d6, 298 K) : δ 7.10 (m, 2H), 5.54-5.38 (m, 14H), 4.80 (m, 6H), 4.62 (dd, J=9.7Hz, J=3.4Hz, 1H), 4.53-4.47 (m, 3H), 4.44-4.38 (m, 1H), 4.32-4.21 (m, 6H), 3.85-3.53 (m, 28H), 3.47-3.34 (m, overlapped with water peak), 3.08-2.99 (m, 1H), 2.53.(s, overlapped with DSMO peak), 2.29 (s, 3H) ; MALDI-TOF: 1340.5 D (calcul. for M+Na+ 1340.2 D).

A. Khawam, D. R. Flanagan, J. Phys. Chem. B 2006, 110, 17315-17328.