Supporting Information

for

In vivo toxicity evaluation of boron nitride nanosheets with different sizes by silkworm model

Vivian Andoh ‡1, Hai-Yan Liu ‡2, Lin Ma1*

Address: 1 College of Biotechnology, Jiangsu University of Science and Technology, Zhenjiang 212000, China 2 College of Tea and Food Science Technology, Jiangsu Vocational College of Agriculture and Forestry, Jurong 212400, China

Email: Lin Ma - ma_lin_1988@126.com

* Corresponding author

‡ Equal contributors

# Results and Discussions

- Size distribution of BN NSs

Figure S1: Size distribution of BN NSs-1 a) and BN NSs-2 b).

Statistical Analysis

Table S1: The data of silkworm larvae (qiufeng × baiyu) weight from different groups (g) (0 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.584 | 0.524 | 0.576 |
| 2 | 0.619 | 0.569 | 0.529 |
| 3 | 0.56 | 0.556 | 0.578 |
| 4 | 0.527 | 0.6 | 0.66 |
| 5 | 0.618 | 0.606 | 0.517 |
| 6 | 0.565 | 0.532 | 0.608 |
| 7 | 0.575 | 0.55 | 0.653 |
| 8 | 0.739 | 0.533 | 0.511 |
| 9 | 0.613 | 0.542 | 0.687 |
| 10 | 0.538 | 0.524 | 0.622 |
| 11 | 0.583 | 0.595 | 0.677 |
| 12 | 0.582 | 0.539 | 0.54 |
| 13 | 0.547 | 0.553 | 0.678 |
| 14 | 0.541 | 0.504 | 0.534 |
| 15 | 0.522 | 0.597 | 0.591 |
| 16 | 0.698 | 0.533 | 0.519 |
| 17 | 0.542 | 0.539 | 0.692 |
| 18 | 0.508 | 0.545 | 0.53 |
| 19 | 0.501 | 0.572 | 0.574 |
| 20 | 0.556 | 0.546 | 0.607 |
| Average | 0.5759 | 0.55295 | 0.59415 |
| Standard deviation | 0.058135101 | 0.0276613 | 0.061421718 |

Table S2: The data of silkworm larvae (qiufeng × baiyu) weight from different groups (g) (24 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.95 | 0.925 | 1.185 |
| 2 | 0.903 | 0.934 | 1.044 |
| 3 | 0.939 | 0.949 | 1.218 |
| 4 | 1.012 | 0.909 | 1.101 |
| 5 | 1.021 | 0.962 | 0.982 |
| 6 | 0.935 | 0.93 | 1.197 |
| 7 | 1.152 | 0.943 | 0.987 |
| 8 | 1.085 | 1.041 | 1.297 |
| 9 | 1.068 | 0.85 | 1.161 |
| 10 | 0.925 | 0.91 | 1.005 |
| 11 | 1.093 | 0.873 | 1.192 |
| 12 | 0.954 | 0.817 | 0.966 |
| 13 | 1.001 | 0.894 | 1.097 |
| 14 | 1.006 | 0.879 | 1.092 |
| 15 | 1.033 | 0.866 | 0.927 |
| 16 | 1.302 | 0.872 | 1.314 |
| 17 | 1.061 | 0.879 | 0.933 |
| 18 | 1.013 | 0.821 | 1.218 |
| 19 | 1.175 | 0.866 | 0.968 |
| 20 | 1.18 | 0.899 | 0.995 |
| Average | 1.0404 | 0.90095 | 1.09395 |
| Standard deviation | 0.099595381 | 0.050592959 | 0.119098898 |

Table S3: The data of silkworm larvae (qiufeng × baiyu) weight from different groups (g) (48 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 1.681 | 1.556 | 1.601 |
| 2 | 1.734 | 1.406 | 1.635 |
| 3 | 1.72 | 1.623 | 1.736 |
| 4 | 1.517 | 1.684 | 1.517 |
| 5 | 1.917 | 1.578 | 1.898 |
| 6 | 1.881 | 1.708 | 1.846 |
| 7 | 1.563 | 1.572 | 1.597 |
| 8 | 1.521 | 1.637 | 1.713 |
| 9 | 1.602 | 1.696 | 1.74 |
| 10 | 1.843 | 1.619 | 1.947 |
| 11 | 1.601 | 1.562 | 1.72 |
| 12 | 1.541 | 1.478 | 1.501 |
| 13 | 1.614 | 1.627 | 1.736 |
| 14 | 1.502 | 1.59 | 1.923 |
| 15 | 1.547 | 1.555 | 1.528 |
| 16 | 1.484 | 1.697 | 1.529 |
| 17 | 1.456 | 1.602 | 1.81 |
| 18 | 1.604 | 1.632 | 1.472 |
| 19 | 1.442 | 1.576 | 1.42 |
| 20 | 1.481 | 1.795 | 1.425 |
| Average | 1.61255 | 1.60965 | 1.6647 |
| Standard deviation | 0.137512354 | 0.082883216 | 0.16213516 |

Table S4: The data of silkworm larvae (qiufeng × baiyu) weight from different groups (g) (72 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 2.675 | 2.654 | 2.788 |
| 2 | 2.369 | 2.436 | 2.583 |
| 3 | 2.502 | 2.561 | 2.472 |
| 4 | 2.295 | 2.495 | 2.559 |
| 5 | 2.363 | 2.531 | 2.333 |
| 6 | 2.709 | 2.394 | 2.71 |
| 7 | 2.229 | 2.352 | 2.603 |
| 8 | 2.444 | 2.658 | 2.472 |
| 9 | 2.348 | 2.33 | 2.597 |
| 10 | 2.265 | 2.673 | 2.396 |
| 11 | 2.401 | 2.443 | 2.406 |
| 12 | 2.252 | 2.41 | 2.386 |
| 13 | 2.34 | 2.645 | 2.649 |
| 14 | 2.313 | 2.603 | 2.601 |
| 15 | 2.35 | 2.38 | 2.569 |
| 16 | 2.55 | 2.529 | 2.677 |
| 17 | 2.228 | 2.529 | 2.328 |
| 18 | 2.203 | 2.634 | 2.306 |
| 19 | 2.503 | 2.305 | 2.314 |
| 20 | 2.276 | 2.666 | 2.302 |
| Average | 2.38075 | 2.5114 | 2.50255 |
| Standard deviation | 0.140002098 | 0.120302702 | 0.146444349 |

Table S5: The data of silkworm larvae (qiufeng × baiyu) weight from different groups (g) (96 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 2.676 | 2.971 | 3.226 |
| 2 | 2.931 | 3.066 | 3.008 |
| 3 | 3.239 | 3.235 | 2.754 |
| 4 | 2.84 | 2.852 | 3.23 |
| 5 | 3.38 | 3.219 | 2.731 |
| 6 | 2.824 | 3.011 | 3.058 |
| 7 | 2.933 | 3.147 | 3.05 |
| 8 | 3.075 | 3.122 | 3.175 |
| 9 | 3.04 | 2.972 | 2.946 |
| 10 | 3.078 | 2.852 | 3.34 |
| 11 | 2.993 | 3.248 | 3.251 |
| 12 | 2.952 | 3.193 | 3.217 |
| 13 | 2.951 | 2.852 | 2.905 |
| 14 | 2.908 | 3.26 | 2.955 |
| 15 | 2.838 | 3.229 | 3.183 |
| 16 | 2.769 | 3 | 3.137 |
| 17 | 2.685 | 2.857 | 3.082 |
| 18 | 2.905 | 3.127 | 2.853 |
| 19 | 2.909 | 3.277 | 3.358 |
| 20 | 2.716 | 3.144 | 3.106 |
| Average | 2.9321 | 3.0817 | 3.07825 |
| Standard deviation | 0.170797219 | 0.146770603 | 0.17472718 |

Figure S2: One sample Kolmogorov-Smirnov Test for the data of silkworm larvae (qiufeng × baiyu) weight.

Table S6: Kruskal Wallis Test for the data of silkworm larvae (qiufeng × baiyu) weight from different groups (g) by changing time

|  |  | Number | Average grade | X2 | df | Progressive significance |
| --- | --- | --- | --- | --- | --- | --- |
| 0h | Control | 20 | 31.25 | 3.568 | 2 | 0.168 |
|  | G1 | 20 | 24.95 |  |  |  |
|  | G2 | 20 | 35.30 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 24h | Control | 20 | 36.28 | 31.191 | 2 | 0 |
|  | G1 | 20 | 13.03 |  |  |  |
|  | G2 | 20 | 42.20 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 48h | Control | 20 | 27.35 | 1.555 | 2 | 0.46 |
|  | G1 | 20 | 29.98 |  |  |  |
|  | G2 | 20 | 34.18 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 72h | Control | 20 | 20.65 | 9.639 | 2 | 0.008 |
|  | G1 | 20 | 36.28 |  |  |  |
|  | G2 | 20 | 34.58 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 96h | Control | 20 | 20.63 | 9.615 | 2 | 0.008 |
|  | G1 | 20 | 35.85 |  |  |  |
|  | G2 | 20 | 35.03 |  |  |  |
|  | Total | 60 |  |  |  |  |

Note: When the degree of freedom (df) is 2, and the confidence level (α) is 0.05, the critical value of X2 is 5.991 by referring to the X2 distribution critical value table. X2 value is less than 5.991, and progressive significance-value is larger than 0.05, indicating that the conclusion is to accept the null hypothesis, and there is no significant difference among the three groups. X2 value is larger than 5.991, and progressive significance-value is less than 0.05, indicating that the conclusion is to reject the null hypothesis, and there is significant difference among the three groups.

Table S7: The data of silkworm larvae (Nistari 7019) weight from different groups (g) (0 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.417 | 0.417 | 0.46 |
| 2 | 0.367 | 0.518 | 0.358 |
| 3 | 0.394 | 0.494 | 0.445 |
| 4 | 0.394 | 0.417 | 0.432 |
| 5 | 0.334 | 0.441 | 0.501 |
| 6 | 0.433 | 0.428 | 0.378 |
| 7 | 0.431 | 0.454 | 0.356 |
| 8 | 0.42 | 0.458 | 0.432 |
| 9 | 0.436 | 0.474 | 0.387 |
| 10 | 0.44 | 0.459 | 0.482 |
| 11 | 0.388 | 0.464 | 0.461 |
| 12 | 0.451 | 0.461 | 0.466 |
| 13 | 0.358 | 0.426 | 0.419 |
| 14 | 0.42 | 0.375 | 0.413 |
| 15 | 0.395 | 0.406 | 0.413 |
| 16 | 0.445 | 0.453 | 0.465 |
| 17 | 0.385 | 0.388 | 0.339 |
| 18 | 0.397 | 0.411 | 0.383 |
| 19 | 0.402 | 0.438 | 0.395 |
| 20 | 0.434 | 0.343 | 0.398 |
| Average | 0.40705 | 0.43625 | 0.41915 |
| Standard deviation | 0.030422812 | 0.03979934 | 0.043963934 |

Table S8: The data of silkworm larvae (Nistari 7019) weight from different groups (g) (24 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.548 | 0.526 | 0.539 |
| 2 | 0.462 | 0.486 | 0.593 |
| 3 | 0.554 | 0.615 | 0.522 |
| 4 | 0.62 | 0.527 | 0.555 |
| 5 | 0.522 | 0.552 | 0.518 |
| 6 | 0.597 | 0.612 | 0.575 |
| 7 | 0.559 | 0.633 | 0.492 |
| 8 | 0.557 | 0.667 | 0.643 |
| 9 | 0.513 | 0.614 | 0.483 |
| 10 | 0.489 | 0.559 | 0.549 |
| 11 | 0.428 | 0.594 | 0.518 |
| 12 | 0.6 | 0.498 | 0.544 |
| 13 | 0.571 | 0.53 | 0.631 |
| 14 | 0.479 | 0.543 | 0.52 |
| 15 | 0.509 | 0.542 | 0.561 |
| 16 | 0.588 | 0.53 | 0.587 |
| 17 | 0.528 | 0.547 | 0.628 |
| 18 | 0.559 | 0.632 | 0.588 |
| 19 | 0.593 | 0.545 | 0.54 |
| 20 | 0.583 | 0.519 | 0.562 |
| Average | 0.54295 | 0.56355 | 0.5574 |
| Standard deviation | 0.049687498 | 0.048800077 | 0.043369805 |

Table S9: The data of silkworm larvae (Nistari 7019) weight from different groups (g) (48 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.767 | 0.786 | 0.882 |
| 2 | 0.611 | 0.896 | 0.851 |
| 3 | 0.801 | 0.903 | 0.797 |
| 4 | 0.782 | 0.863 | 0.846 |
| 5 | 0.884 | 0.756 | 0.807 |
| 6 | 0.719 | 0.75 | 0.848 |
| 7 | 0.813 | 0.818 | 0.878 |
| 8 | 0.842 | 0.717 | 0.816 |
| 9 | 0.838 | 0.761 | 0.781 |
| 10 | 0.772 | 0.723 | 0.917 |
| 11 | 0.859 | 0.766 | 0.898 |
| 12 | 0.791 | 0.786 | 0.864 |
| 13 | 0.769 | 0.841 | 0.754 |
| 14 | 0.816 | 0.759 | 0.891 |
| 15 | 0.782 | 0.806 | 0.884 |
| 16 | 0.793 | 0.792 | 0.811 |
| 17 | 0.755 | 0.857 | 0.846 |
| 18 | 0.765 | 0.777 | 0.848 |
| 19 | 0.743 | 0.787 | 0.781 |
| 20 | 0.811 | 0.819 | 0.81 |
| Average | 0.78565 | 0.79815 | 0.8405 |
| Standard deviation | 0.055931454 | 0.051060038 | 0.043326089 |

Table S10: The data of silkworm larvae (Nistari 7019) weight from different groups (g) (72 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.993 | 1.052 | 0.973 |
| 2 | 1.147 | 1.094 | 1.104 |
| 3 | 1.037 | 1.037 | 1.174 |
| 4 | 1.096 | 1.034 | 1.104 |
| 5 | 1.144 | 1.114 | 1.154 |
| 6 | 1.07 | 1.118 | 1.12 |
| 7 | 1.077 | 0.982 | 1.08 |
| 8 | 1.069 | 1.021 | 1.178 |
| 9 | 1.094 | 0.968 | 1.055 |
| 10 | 1.045 | 0.94 | 1.087 |
| 11 | 1 | 0.968 | 0.998 |
| 12 | 1.052 | 0.975 | 0.987 |
| 13 | 1.02 | 0.95 | 0.969 |
| 14 | 1.064 | 0.953 | 0.996 |
| 15 | 1.062 | 0.987 | 0.997 |
| 16 | 1.015 | 0.942 | 1.064 |
| 17 | 1.032 | 0.991 | 1.082 |
| 18 | 0.989 | 0.956 | 1.028 |
| 19 | 0.989 | 0.943 | 1.132 |
| 20 | 1.12 | 0.913 | 1.049 |
| Average | 1.05575 | 0.9969 | 1.06655 |
| Standard deviation | 0.047012631 | 0.058697445 | 0.064591389 |

Table S11: The data of silkworm larvae (Nistari 7019) weight from different groups (g) (96 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 1.385 | 1.168 | 1.185 |
| 2 | 1.339 | 1.312 | 1.188 |
| 3 | 1.194 | 1.166 | 1.374 |
| 4 | 1.296 | 1.182 | 1.22 |
| 5 | 1.187 | 1.271 | 1.331 |
| 6 | 1.332 | 1.282 | 1.286 |
| 7 | 1.23 | 1.302 | 1.365 |
| 8 | 1.265 | 1.21 | 1.351 |
| 9 | 1.171 | 1.128 | 1.436 |
| 10 | 1.232 | 1.175 | 1.144 |
| 11 | 1.281 | 1.157 | 1.171 |
| 12 | 1.184 | 1.184 | 1.255 |
| 13 | 1.2 | 1.329 | 1.277 |
| 14 | 1.174 | 1.133 | 1.313 |
| 15 | 1.308 | 1.127 | 1.358 |
| 16 | 1.167 | 1.221 | 1.302 |
| 17 | 1.37 | 1.107 | 1.476 |
| 18 | 1.136 | 1.111 | 1.17 |
| 19 | 1.259 | 1.144 | 1.211 |
| 20 | 1.132 | 1.127 | 1.249 |
| Average | 1.2421 | 1.1918 | 1.2831 |
| Standard deviation | 0.075259484 | 0.069217483 | 0.090520108 |

Figure S3: One sample Kolmogorov-Smirnov Test for the data of silkworm larvae (Nistari 7019) weight.

Table S12: Kruskal Wallis Test for the data of silkworm larvae (Nistari 7019) weight from different groups (g) by changing time

|  |  | Number | Average grade | X2 | df | Progressive significance |
| --- | --- | --- | --- | --- | --- | --- |
| 0h | Control | 20 | 24.60 | 5.032 | 2 | 0.081 |
|  | G1 | 20 | 36.95 |  |  |  |
|  | G2 | 20 | 29.95 |  |  |  |
|  | Total | 60 | - |  |  |  |
| 24h | Control | 20 | 27.93 | 0.739 | 2 | 0.691 |
|  | G1 | 20 | 32.60 |  |  |  |
|  | G2 | 20 | 30.98 |  |  |  |
|  | Total | 60 | - |  |  |  |
| 48h | Control | 20 | 24.33 | 10.434 | 2 | 0.005 |
|  | G1 | 20 | 26.45 |  |  |  |
|  | G2 | 20 | 40.73 |  |  |  |
|  | Total | 60 | - |  |  |  |
| 72h | Control | 20 | 35.43 | 14.07 | 2 | 0.001 |
|  | G1 | 20 | 18.60 |  |  |  |
|  | G2 | 20 | 37.48 |  |  |  |
|  | Total | 60 | - |  |  |  |
| 96h | Control | 20 | 32.20 | 11.568 | 2 | 0.003 |
|  | G1 | 20 | 20.38 |  |  |  |
|  | G2 | 20 | 38.93 |  |  |  |
|  | Total | 60 | - |  |  |  |

Note: When the degree of freedom (df) is 2, and the confidence level (α) is 0.05, the critical value of X2 is 5.991 by referring to the X2 distribution critical value table. X2 value is less than 5.991, and progressive significance-value is larger than 0.05, indicating that the conclusion is to accept the null hypothesis, and there is no significant difference among the three groups. X2 value is larger than 5.991, and progressive significance-value is less than 0.05, indicating that the conclusion is to reject the null hypothesis, and there is significant difference among the three groups.

Table S13: The data of silkworm larvae (qiufeng × baiyu) length from different groups (cm) (0 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 4.2 | 4.2 | 4.1 |
| 2 | 4.3 | 4.1 | 4 |
| 3 | 4.2 | 3.8 | 4.4 |
| 4 | 4 | 4.2 | 4 |
| 5 | 4.1 | 4 | 4.2 |
| 6 | 4 | 4.1 | 3.9 |
| 7 | 4.2 | 4 | 4.3 |
| 8 | 4.1 | 3.9 | 4 |
| 9 | 4.2 | 4 | 4 |
| 10 | 3.9 | 4 | 4.2 |
| 11 | 4 | 4 | 4.4 |
| 12 | 4.1 | 4.1 | 4.4 |
| 13 | 3.9 | 4.2 | 4 |
| 14 | 4 | 3.9 | 4.1 |
| 15 | 4 | 3.8 | 3.9 |
| 16 | 4 | 4 | 4.1 |
| 17 | 4.2 | 4 | 3.9 |
| 18 | 4 | 4 | 4 |
| 19 | 4.1 | 3.8 | 4 |
| 20 | 4.3 | 3.8 | 3.8 |
| Average | 4.09 | 3.995 | 4.085 |
| Standard deviation | 0.117898261 | 0.128354977 | 0.173997126 |

Table S14: The data of silkworm larvae (qiufeng × baiyu) length from different groups (cm) (24 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 5.3 | 4.7 | 5.3 |
| 2 | 5.1 | 4.7 | 5.4 |
| 3 | 5.2 | 4.8 | 4.9 |
| 4 | 5.1 | 5 | 5 |
| 5 | 4.6 | 4.7 | 5 |
| 6 | 4.9 | 4.6 | 5.4 |
| 7 | 4.9 | 4.8 | 5.2 |
| 8 | 5 | 4.6 | 4.8 |
| 9 | 4.9 | 4.8 | 5.4 |
| 10 | 5.4 | 5 | 5.3 |
| 11 | 4.9 | 4.7 | 5.1 |
| 12 | 5 | 4.7 | 4.8 |
| 13 | 4.9 | 4.5 | 5.1 |
| 14 | 4.8 | 4.7 | 5 |
| 15 | 4.9 | 4.6 | 5.3 |
| 16 | 5 | 4.6 | 4.9 |
| 17 | 4.8 | 5 | 5.2 |
| 18 | 4.8 | 4.7 | 4.8 |
| 19 | 4.7 | 4.7 | 4.6 |
| 20 | 4.9 | 4.8 | 4.8 |
| Average | 4.955 | 4.735 | 5.065 |
| Standard deviation | 0.188348082 | 0.135185058 | 0.235106359 |

Table S15: The data of silkworm larvae (qiufeng × baiyu) length from different groups (cm) (48 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 6.2 | 5.9 | 5.9 |
| 2 | 5.8 | 5.7 | 5.6 |
| 3 | 5.7 | 5.8 | 5.5 |
| 4 | 5.6 | 5.6 | 5.8 |
| 5 | 5.7 | 6 | 5.5 |
| 6 | 6.3 | 5.7 | 5.9 |
| 7 | 6.3 | 5.8 | 5.8 |
| 8 | 5.8 | 5.5 | 5.8 |
| 9 | 5.5 | 5.8 | 5.7 |
| 10 | 5.5 | 5.5 | 5.6 |
| 11 | 5.9 | 5.8 | 5.7 |
| 12 | 5.4 | 5.4 | 5.8 |
| 13 | 5.7 | 5.4 | 6.1 |
| 14 | 5.5 | 5.7 | 5.8 |
| 15 | 5.5 | 5.6 | 5.6 |
| 16 | 5.8 | 5.6 | 5.5 |
| 17 | 5.6 | 5.5 | 6.2 |
| 18 | 5.7 | 5.6 | 6.2 |
| 19 | 5.7 | 5.5 | 6 |
| 20 | 5.6 | 5.5 | 5.4 |
| Average | 5.74 | 5.645 | 5.77 |
| Standard deviation | 0.253771551 | 0.162711401 | 0.226053091 |

Table S16: The data of silkworm larvae (qiufeng × baiyu) length from different groups (cm) (72 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 6.5 | 6.5 | 7 |
| 2 | 6.6 | 6.6 | 6.7 |
| 3 | 6.5 | 6.8 | 6.7 |
| 4 | 6.4 | 6.5 | 6.7 |
| 5 | 6.3 | 6.3 | 6.5 |
| 6 | 6.4 | 6.5 | 6.6 |
| 7 | 6.3 | 6.4 | 6.4 |
| 8 | 6.3 | 6.6 | 6.4 |
| 9 | 6.7 | 6.4 | 6.6 |
| 10 | 6.5 | 6.8 | 6.2 |
| 11 | 6.5 | 6.7 | 6.4 |
| 12 | 6.3 | 6.6 | 6.3 |
| 13 | 6.3 | 6.4 | 6.6 |
| 14 | 6.5 | 6.5 | 6.7 |
| 15 | 6.2 | 6.5 | 6.5 |
| 16 | 6.3 | 6.3 | 6.5 |
| 17 | 6.2 | 6.6 | 6.6 |
| 18 | 6.3 | 6.5 | 6.5 |
| 19 | 6.5 | 6.7 | 6.3 |
| 20 | 6.7 | 6.7 | 6.5 |
| Average | 6.415 | 6.545 | 6.535 |
| Standard deviation | 0.145859521 | 0.14309088 | 0.176847392 |

Table S17: The data of silkworm larvae (qiufeng × baiyu) length from different groups (cm) (96 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 7.1 | 6.9 | 7 |
| 2 | 6.8 | 7.1 | 7.2 |
| 3 | 6.8 | 7.1 | 6.7 |
| 4 | 6.5 | 6.8 | 7 |
| 5 | 6.8 | 6.7 | 6.9 |
| 6 | 6.7 | 7.1 | 6.9 |
| 7 | 6.6 | 6.6 | 6.7 |
| 8 | 6.8 | 7 | 7.1 |
| 9 | 7 | 6.7 | 7.1 |
| 10 | 7 | 6.8 | 6.9 |
| 11 | 6.9 | 7 | 7 |
| 12 | 6.7 | 7.1 | 6.7 |
| 13 | 6.8 | 6.6 | 6.8 |
| 14 | 6.7 | 7.2 | 6.8 |
| 15 | 6.8 | 7 | 7 |
| 16 | 6.7 | 6.9 | 6.9 |
| 17 | 6.6 | 7 | 6.7 |
| 18 | 6.4 | 7 | 7.2 |
| 19 | 6.8 | 6.8 | 6.9 |
| 20 | 6.8 | 6.6 | 7 |
| Average | 6.765 | 6.9 | 6.925 |
| Standard deviation | 0.162095651 | 0.184390889 | 0.154515371 |

Figure S4: One sample Kolmogorov-Smirnov Test for the data of silkworm larvae (qiufeng × baiyu) length.

Table S18: Kruskal Wallis Test for the data of silkworm larvae (qiufeng × baiyu) length from different groups (cm) by changing time

|  |  | Number | Average grade | X2 | df | Progressive significance |
| --- | --- | --- | --- | --- | --- | --- |
| 0h | Control | 20 | 35.00 | 4.355 | 2 | 0.113 |
|  | G1 | 20 | 24.25 |  |  |  |
|  | G2 | 20 | 32.25 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 24h | Control | 20 | 34.43 | 21.544 | 2 | 0 |
|  | G1 | 20 | 16.30 |  |  |  |
|  | G2 | 20 | 40.78 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 48h | Control | 20 | 31.03 | 2.923 | 2 | 0.232 |
|  | G1 | 20 | 25.60 |  |  |  |
|  | G2 | 20 | 34.88 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 72h | Control | 20 | 22.00 | 7.479 | 2 | 0.024 |
|  | G1 | 20 | 35.58 |  |  |  |
|  | G2 | 20 | 33.93 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 96h | Control | 20 | 21.63 | 8.102 | 2 | 0.017 |
|  | G1 | 20 | 33.93 |  |  |  |
|  | G2 | 20 | 35.95 |  |  |  |
|  | Total | 60 |  |  |  |  |

Note: When the degree of freedom (df) is 2, and the confidence level (α) is 0.05, the critical value of X2 is 5.991 by referring to the X2 distribution critical value table. X2 value is less than 5.991, and progressive significance-value is larger than 0.05, indicating that the conclusion is to accept the null hypothesis, and there is no significant difference among the three groups. X2 value is larger than 5.991, and progressive significance-value is less than 0.05, indicating that the conclusion is to reject the null hypothesis, and there is significant difference among the three groups.

Table S19: The data of silkworm larvae (Nistari 7019) length from different groups (cm) (0 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 3.7 | 4 | 3.9 |
| 2 | 3.8 | 3.9 | 4 |
| 3 | 3.7 | 4 | 3.9 |
| 4 | 3.7 | 4 | 3.8 |
| 5 | 3.8 | 3.7 | 3.9 |
| 6 | 4 | 3.9 | 3.9 |
| 7 | 3.7 | 3.5 | 3.9 |
| 8 | 3.9 | 4 | 3.7 |
| 9 | 3.8 | 4 | 4 |
| 10 | 3.7 | 3.7 | 3.7 |
| 11 | 4 | 3 | 3.6 |
| 12 | 3.7 | 3.9 | 4 |
| 13 | 3.9 | 4 | 4.1 |
| 14 | 4 | 3.9 | 3.7 |
| 15 | 3.7 | 3.9 | 3.9 |
| 16 | 3.9 | 3.7 | 4 |
| 17 | 3.8 | 3.8 | 3.7 |
| 18 | 3.7 | 4 | 3.8 |
| 19 | 3.7 | 4 | 3.9 |
| 20 | 4 | 3.8 | 3.9 |
| Average | 3.81 | 3.835 | 3.865 |
| Standard deviation | 0.117898261 | 0.235106359 | 0.127573508 |

Table S20: The data of silkworm larvae (Nistari 7019) length from different groups (cm) (24 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 3.9 | 4.6 | 4.5 |
| 2 | 4.4 | 4.5 | 4.4 |
| 3 | 4.3 | 4.6 | 4.1 |
| 4 | 4.3 | 4.1 | 4.4 |
| 5 | 4.6 | 4.5 | 4.2 |
| 6 | 3.9 | 4.5 | 4.4 |
| 7 | 4.2 | 4.1 | 4.4 |
| 8 | 4.2 | 4 | 4.4 |
| 9 | 4.3 | 4.5 | 4.3 |
| 10 | 4.2 | 4.5 | 4.5 |
| 11 | 4.4 | 4.5 | 4.5 |
| 12 | 4.1 | 4.2 | 4.1 |
| 13 | 3.9 | 4.5 | 4.5 |
| 14 | 4.2 | 4.1 | 4.2 |
| 15 | 4.2 | 4.6 | 4.5 |
| 16 | 4 | 4.3 | 4.5 |
| 17 | 4 | 4.5 | 4.5 |
| 18 | 4.1 | 4.6 | 4.1 |
| 19 | 4.2 | 4.2 | 4.2 |
| 20 | 4.1 | 4.4 | 4.3 |
| Average | 4.175 | 4.39 | 4.35 |
| Standard deviation | 0.178535711 | 0.194679223 | 0.146628783 |

Table S21: The data of silkworm larvae (Nistari 7019) length from different groups (cm) (48 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 5 | 5 | 5.1 |
| 2 | 5 | 5 | 5.1 |
| 3 | 5 | 5 | 5.1 |
| 4 | 4.9 | 4.7 | 5 |
| 5 | 5.1 | 5 | 5 |
| 6 | 5 | 4.9 | 5.1 |
| 7 | 5 | 5.1 | 5 |
| 8 | 5 | 5 | 5 |
| 9 | 5.1 | 5.1 | 5 |
| 10 | 5 | 5 | 5.1 |
| 11 | 5 | 5 | 5 |
| 12 | 5 | 5 | 4.9 |
| 13 | 4.9 | 5 | 5.1 |
| 14 | 5 | 4.9 | 5 |
| 15 | 5 | 5 | 5 |
| 16 | 4.9 | 5.2 | 5 |
| 17 | 5 | 5 | 5 |
| 18 | 4.6 | 5 | 5 |
| 19 | 5 | 5 | 5 |
| 20 | 5 | 5.1 | 5 |
| Average | 4.975 | 5 | 5.025 |
| Standard deviation | 0.099373035 | 0.09486833 | 0.053619026 |

Table S22: The data of silkworm larvae (Nistari 7019) length from different groups (cm) (72 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 5.2 | 5.3 | 5.7 |
| 2 | 5.5 | 5.2 | 5.7 |
| 3 | 5.1 | 5.3 | 5.5 |
| 4 | 5.2 | 5.5 | 5.5 |
| 5 | 5.3 | 5.2 | 5.2 |
| 6 | 5.3 | 5.3 | 5.2 |
| 7 | 5.2 | 5.4 | 5.2 |
| 8 | 5.4 | 5.1 | 5.5 |
| 9 | 5.3 | 5.5 | 5.3 |
| 10 | 5.3 | 5.1 | 5.4 |
| 11 | 5.5 | 5.2 | 5.3 |
| 12 | 5.2 | 5.3 | 5.6 |
| 13 | 5.5 | 5.2 | 5.3 |
| 14 | 5.4 | 5.3 | 5.5 |
| 15 | 5.5 | 5.3 | 5.4 |
| 16 | 5.4 | 5.2 | 5.5 |
| 17 | 5.4 | 5.2 | 5.3 |
| 18 | 5.6 | 5.7 | 5.5 |
| 19 | 5.4 | 5.3 | 5.4 |
| 20 | 5.5 | 5.3 | 5.3 |
| Average | 5.36 | 5.295 | 5.415 |
| Standard deviation | 0.13190906 | 0.139552857 | 0.149248116 |

Table S23: The data of silkworm larvae (Nistari 7019) length from different groups (cm) (96 h)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 5.6 | 5.7 | 6 |
| 2 | 5.7 | 5.7 | 5.7 |
| 3 | 5.7 | 5.8 | 5.7 |
| 4 | 5.6 | 5.8 | 5.8 |
| 5 | 5.7 | 5.6 | 5.7 |
| 6 | 5.7 | 5.7 | 6 |
| 7 | 6 | 5.7 | 5.7 |
| 8 | 5.6 | 5.6 | 5.8 |
| 9 | 5.7 | 5.7 | 6 |
| 10 | 5.6 | 5.6 | 5.9 |
| 11 | 5.7 | 5.7 | 6 |
| 12 | 5.7 | 5.6 | 5.6 |
| 13 | 5.7 | 5.7 | 5.6 |
| 14 | 5.7 | 5.8 | 5.8 |
| 15 | 5.8 | 5.6 | 5.6 |
| 16 | 5.8 | 5.9 | 5.7 |
| 17 | 5.6 | 5.7 | 5.7 |
| 18 | 5.6 | 5.7 | 5.7 |
| 19 | 5.7 | 5.6 | 5.8 |
| 20 | 5.7 | 5.7 | 5.8 |
| Average | 5.695 | 5.695 | 5.78 |
| Standard deviation | 0.092059763 | 0.080467385 | 0.132664992 |

Figure S5: One sample Kolmogorov-Smirnov Test for the data of silkworm larvae (Nistari 7019) length.

Table S24: Kruskal Wallis Test for the data of silkworm larvae (Nistari 7019) length from different groups (cm) by changing time

|  |  | Number | Average grade | X2 | df | Progressive significance |
| --- | --- | --- | --- | --- | --- | --- |
| 0h | Control | 20 | 25.50 | 2.682 | 2 | 0.262 |
|  | G1 | 20 | 33.70 |  |  |  |
|  | G2 | 20 | 32.30 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 24h | Control | 20 | 19.73 | 12.423 | 2 | 0.002 |
|  | G1 | 20 | 38.10 |  |  |  |
|  | G2 | 20 | 33.68 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 48h | Control | 20 | 26.23 | 3.631 | 2 | 0.163 |
|  | G1 | 20 | 30.28 |  |  |  |
|  | G2 | 20 | 35.00 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 72h | Control | 20 | 31.68 | 6.81 | 2 | 0.033 |
|  | G1 | 20 | 22.95 |  |  |  |
|  | G2 | 20 | 36.88 |  |  |  |
|  | Total | 60 |  |  |  |  |
| 96h | Control | 20 | 26.38 | 6.284 | 2 | 0.043 |
|  | G1 | 20 | 27.15 |  |  |  |
|  | G2 | 20 | 37.98 |  |  |  |
|  | Total | 60 | - |  |  |  |

Note: When the degree of freedom (df) is 2, and the confidence level (α) is 0.05, the critical value of X2 is 5.991 by referring to the X2 distribution critical value table. X2 value is less than 5.991, and progressive significance-value is larger than 0.05, indicating that the conclusion is to accept the null hypothesis, and there is no significant difference among the three groups. X2 value is larger than 5.991, and progressive significance-value is less than 0.05, indicating that the conclusion is to reject the null hypothesis, and there is significant difference among the three groups.

- The concentration effect of BN NSs toxicity

Figure S6: The effect of BN NSs-1 on the growth of silkworms (qiufeng × baiyu). a, b, c) The pictures of silkworm larvae after the intake of BN NSs-1 for different times (a: control, b: 2% BN NSs-1, c: 8% BN NSs-1). d, e) The comparison of the average length (AL, d) and weight (AW, e) and of silkworm larvae from different groups, the error bars stand for the standard deviation of AW and AL respectively.

Figure S7: The effect of BN NSs-2 on the growth of silkworms (qiufeng × baiyu). a, b, c) The pictures of silkworm larvae after the intake of BN NSs-2 for different times (a: control, b: 2% BN NSs-2, c: 8% BN NSs-2). d, e) The comparison of the average length (AL, d) and weight (AW, e) and of silkworm larvae from different groups, the error bars stand for the standard deviation of AW and AL respectively.

- The food intake speed of silkworms

In order to study the food intake speed of silkworms, the weight of mulberry leaves eaten by silkworms every day was recorded, taking qiufeng × baiyu as example and using two concentrations (2% and 8%) of BN NSs-1 and BN NSs-2. The data in Table S25 shows that there is a certain difference among different groups in the food intake speed of silkworms, but it is not very obvious. More studies on the food intake speed of each silkworm in every group should be carried out in the future.

Table S25: The raw data of weight of mulberry leaves eaten by silkworms (qiufeng × baiyu) (g)

|  | control | BN NSs-1 |  | BN NSs-2 |  |
| --- | --- | --- | --- | --- | --- |
|  |  | 2% | 8% | 2% | 8% |
| 1st | 47.47 | 47.96 | 46.45 | 51.44 | 44.83 |
| 2nd | 42.02 | 46.1 | 49.61 | 48.48 | 47.24 |
| 3rd | 43.51 | 43.32 | 43.77 | 44.73 | 43.75 |
| 4th | 46.89 | 49.96 | 45.29 | 46.28 | 43.94 |

Table S26: The data of cocoon (qiufeng × baiyu) weight from different groups (g)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.507 | 0.562 | 0.524 |
| 2 | 0.473 | 0.549 | 0.593 |
| 3 | 0.535 | 0.499 | 0.536 |
| 4 | 0.567 | 0.529 | 0.578 |
| 5 | 0.542 | 0.547 | 0.548 |
| 6 | 0.566 | 0.507 | 0.523 |
| 7 | 0.384 | 0.567 | 0.524 |
| 8 | 0.429 | 0.566 | 0.545 |
| 9 | 0.484 | 0.531 | 0.529 |
| 10 | 0.466 | 0.569 | 0.525 |
| 11 | 0.558 | 0.57 | 0.603 |
| 12 | 0.449 | 0.538 | 0.54 |
| 13 | 0.526 | 0.574 | 0.525 |
| 14 | 0.353 | 0.571 | 0.563 |
| 15 | 0.532 | 0.529 | 0.493 |
| 16 | 0.537 | 0.431 | 0.62 |
| 17 | 0.543 | 0.577 | 0.582 |
| 18 | 0.532 | 0.56 | 0.578 |
| 19 | 0.54 | 0.537 | 0.515 |
| 20 | 0.567 | 0.532 | 0.601 |
| Standard deviation | 0.061 | 0.034 | 0.035 |
| Average | 0.505 | 0.542 | 0.552 |

Table S27: The data of cocoon (Nistari 7019) weight from different groups (g)

| Sample | Control | G1 | G2 |
| --- | --- | --- | --- |
| 1 | 0.196 | 0.211 | 0.254 |
| 2 | 0.214 | 0.216 | 0.311 |
| 3 | 0.224 | 0.259 | 0.241 |
| 4 | 0.213 | 0.274 | 0.249 |
| 5 | 0.232 | 0.224 | 0.223 |
| 6 | 0.225 | 0.203 | 0.236 |
| 7 | 0.282 | 0.229 | 0.254 |
| 8 | 0.253 | 0.208 | 0.234 |
| 9 | 0.248 | 0.223 | 0.259 |
| 10 | 0.237 | 0.204 | 0.203 |
| 11 | 0.249 | 0.227 | 0.279 |
| 12 | 0.252 | 0.208 | 0.234 |
| 13 | 0.237 | 0.205 | 0.258 |
| 14 | 0.203 | 0.213 | 0.214 |
| 15 | 0.232 | 0.218 | 0.268 |
| 16 | 0.241 | 0.258 | 0.265 |
| 17 | 0.204 | 0.254 | 0.240 |
| 18 | 0.248 | 0.271 | 0.201 |
| 19 | 0.204 | 0.247 | 0.202 |
| 20 | 0.212 | 0.202 | 0.202 |
| Standard deviation | 0.022 | 0.024 | 0.029 |
| Average | 0.230 | 0.228 | 0.241 |

Figure S8: One sample Kolmogorov-Smirnov Test for the cocoon weight data from silkworm larvae (qiufeng × baiyu, Nistari 7019).

Table S28: Kruskal Wallis Test for the data of cocoon (qiufeng × baiyu) weight from different groups (g)

|  |  | Number | Average grade | X2 | df | Progressive significance |
| --- | --- | --- | --- | --- | --- | --- |
| Weight | Control | 20 | 22.45 | 6.404 | 2 | 0.041 |
|  | G1 | 20 | 34.08 |  |  |  |
|  | G2 | 20 | 34.98 |  |  |  |
|  | Total | 60 | - |  |  |  |

Note: When the degree of freedom (df) is 2, and the confidence level (α) is 0.05, the critical value of X2 is 5.991 by referring to the X2 distribution critical value table. X2 value is less than 5.991, and progressive significance-value is larger than 0.05, indicating that the conclusion is to accept the null hypothesis, and there is no significant difference among the three groups. X2 value is larger than 5.991, and progressive significance-value is less than 0.05, indicating that the conclusion is to reject the null hypothesis, and there is significant difference among the three groups.

Table S29: Kruskal Wallis Test for the data of cocoon (Nistari 7019) weight from different groups (g)

|  |  | Number | Average grade | X2 | df | Progressive significance |
| --- | --- | --- | --- | --- | --- | --- |
| Weight | Control | 20 | 29.03 | 2.275 | 2 | 0.321 |
|  | G1 | 20 | 27.28 |  |  |  |
|  | G2 | 20 | 35.20 |  |  |  |
|  | Total | 60 | - |  |  |  |

Note: When the degree of freedom (df) is 2, and the confidence level (α) is 0.05, the critical value of X2 is 5.991 by referring to the X2 distribution critical value table. X2 value is less than 5.991, and progressive significance-value is larger than 0.05, indicating that the conclusion is to accept the null hypothesis, and there is no significant difference among the three groups. X2 value is larger than 5.991, and progressive significance-value is less than 0.05, indicating that the conclusion is to reject the null hypothesis, and there is significant difference among the three groups.