Supporting Information

# Improving magnetic properties of Mn and Zn doped core-shell iron oxide nanoparticles by tuning their size

Dounia Louaguef 1, Ghouti Medjahdi1, Sébastien Diliberto1, Klaus M. Seemann1, Thomas Gries1, Joelle Bizeau2, Damien Mertz2, Eric Gaffet1 and  Halima Alem*1

1 Université de Lorraine. CNRS. IJL, F54011 Nancy. France

2 Institut  de physique et de chimie des matériaux. UMR 7504 CNRS – Université de Strasbourg. France

* corresponding author: halima.alem@univ-lorraine.fr

- X- ray diffraction analysis

XRD investigations reveals the structural characterization of the NPs. X-ray patterns of   Zn0.4Fe2,6O4 NPs before and after annealing at 300°C and 700°C are shown in Figure SI 1. The annealing of the nanoparticles at these temperatures was an essential step to eliminate the excess of oleic acid to distinguish the Bragg peaks.

Figure SI 1 . XRD patterns of the as-prepared Zn0.4Fe2,6O4 NPs at 300°C  (Cu kalpha wavelength).

The X-ray diffractograms of the NPs annealed at 300°C (b) show the iron oxide phases of the NPs. They can represent either magnetite (Fe2O3) or maghemite (γ-Fe2O3), because of the similarity of their XRD patterns, it is impossible to make the difference between  the Fe3-O4 magnetite phase from the maghemite phase with the X-Ray analysis36,38. To precise the right phase, the NPs were analyzed by Mössbauer spectroscopy in the next step, we have also compared to the as prepared nanoparticles (Figure 2).

b- Mössbauer spectroscopy:

Mössbauer spectroscopy analysis were performed to determine the NPs phase. The obtained MS spectra of the as-prepared NPs and those annealed at 300 and 700°C are shown in (Figure 2). Their hyperfine parameters are listed in Table 2.

Figure 2 .   Mössbauer spectra of  the as-prepared  Zn0.4Fe2,6O4 NPs (a), annealed NPs  at 300°C  (b),  and at 700°C (c).

The as-prepared NPs Mössbauer (spectrum (a), figure 2) represents one pure doublet which corresponds to the superparamagnetic Fe3O4 NPs  (Iron in oxidation state III). The presence of Fe3+ is also shown in spectrum (spectrum(b),figure 2) which corresponds to NPs annealed at 300°C with a percentage of 65% and the remaining 35% represent Fe2+. On the other hand, the well-defined sextet obtained from the annealed NPs at 700°C (spectrum (c), figure 2) (line width 0.50mm/s) is attributed to Fe metal. The site 1 of this spectrum corresponds to Fe0 and the percentage of this phase is 85%, the sites 2 and 3 correspond to magnetite with a percentage of 8%, finally the site 4 is attributed to 7% of superparamagnetic NPs (see Table 1).

Table 1. The hyperfine parameters of the as-prepared NPs and those annealed at 300 and 700°C obtained from Mössbauer analysis.

| T (°C) | Component (sites) | IS (mm/s) | EQ (mm/s) | B(T) | Phase | Mass(%) |
| --- | --- | --- | --- | --- | --- | --- |
| As Prepared NPs | 1 | 0.33 | 0.69 | - | Fe III | - |
| 300°C | 1 | 0.19 | 0.74 | - | Fe III | 65 |
|  | 2 | 1.24 | 2.28 | - | Fe II | 35 |
| 700°C | 1 | 0 | 0 | 33.1 | Fe0 | 85 |
|  | 2 | 0.29 | 0 | 49 | Fe3-O4 | 8 |
|  | 3 | 0.62 | 0 | 46 |  |  |
|  | 4 | 0.25 | 0 | _ | Fe III | 7 |